TABLE 5-B

MINIMUM REQUIREMENTS FOR STRUCTURAL

COMPOSITION OF PAVEMENTS

Street			Flexible Pavements		Rigid           Pavements

Classification			Alt. #1	Alt. #2

MARGINAL	5” BAM		6” P.C.C.	---------

LAND ACCESS	1 1/2” Class I Surf.	(15’ Plain Jts)

Residential	12” Lime Stab. Subgrade	12” Lime Stab. Subgrade

LOCAL	5” BAM			6” P.C.C.	---------

Residential	1 1/2” Class I Surf.	(15’ Plain Jts)

12” Lime Stab. Subgrade	12” Lime Stab. Subgrade

COLLECTOR	6 1/2” BAM	6” S.R.P.C.C.	6” P.C.C.

Residential	1 1/2” Class I Surf.	(40’ Dowel Jts)	12” Lime Stab. Subgrade

12” Lime Stab. Subgrade	12” Lime Stab. Subgrade

U.L. (15’ Dowel Jts)

LOCAL	4” Bam	7” S.R.P.C.C.	7” P.C.C. (Commercial)

Commercial and	2” Class I Bind.	8” S.R.P.C.C.	8” P.C.C. (Industrial)

Industrial	1 1/2” Class I Surf.	(40’ Dowel Jts)	12” Lime Stab. Subgrade

12” Lime Stab. Subgrade	12” Lime Stab. Subgrade

U.L. (15’ Dowel Jts)

COLLECTOR	6” BAM	8” S.R.P.C.C. (Commercial)

-------------

Commercial and	2 1/2” Class I Bind.	10” S.R.P.C.C. (Industrial)

Industrial	1 1/2” Class I Surf.	(40’ Dowel Jts)

12” Lime Stab. Subgrade	12” Lime Stab. Subgrade

NOTE:	Equivalent pavements in addition to those shown above shall be determined by the Village Engineer.  Should the road pavement thickness exceed 8”, the granular base/ subbase shall extend under the curb/gutter.

ABBREVIATIONS:

Cr. St.		=	Crushed Stone

BAM		=	Bituminous Aggregate Mixture

U.L.		=	Underlayment

P.C.C.		=	Unreinforced Portland Cement Concrete

S.R.P.C.C.	=	Standard Reinforced Portland Cement Concrete

MAXIMUM LIFT THICKNESS:

BAM			=	5”

Class I Binder	=	2 1/2”

Class I Surface	=	1 1/2”